## Slide 1: Comparison of Continuum and Molecular Dynamics Methods for Simulation of Laser Ablation of Metals
<number>
M. Povarnitsyn1, V. Fokin1, P. Levashov1, T. Itina2
1Joint Institute for High Temperatures RAS, Moscow, Russia
2Laboratoire Hubert Curien, St-Etienne, France
povar@ihed.ras.ru
International High Power Laser Ablation and Beamed Energy Propulsion, Santa Fe, USA
22 April 2014

## Slide 2: Outline
Motivation
Brief overview of physics
Numerical models (HD-TTM and MD-TTM)
Results of simulation
Conclusions and outlook
<number>

## Slide 3: Motivation
<number>
Real time and space
LTE?
Nucleation and surface effects?
EOS
Hydrodynamics
Molecular dynamics
V < 1 m3; t ~ 1 ns
Dynamics
Interatomic potential
Potential and ionization?
Notes: <number>

## Slide 4: Goals
Development of HD-TTM and MD-TTM models for simulation of laser-matter interaction
Development of wide-range optical and transport models
Comparison of HD and MD simulation results with experiment
Development of nucleation and fragmentation models based on MD data
<number>

## Slide 5: Stages of ultrafast heating and ablation
t = 0
1. Laser pulse  ~ 100 fs
~10 nm
t < 1 ps
2. CB electrons absorption
~100 nm
t ~ 5 ps
3. Electron heat conductivity +
electron-ion coupling
V > 10 km/s
t > 10 ps
4. Evaporation, shock and rarefaction waves
V ~ 1 km/s
t ~ 100 ps
5. Mechanical fragmentation
V < 1 km/s
<number>
Notes: <number>

## Slide 6
Two-temperature model (TTM)
<number>
Anisimov et al. JETP, 39, 375 (1974)
Notes: <number>

## Slide 7
Two-temperature model (TTM)
<number>
Ivanov & Zhigilei, Phys. Rev. B, 68, 064114 (2003)
Notes: <number>

## Slide 8
Two-temperature hydrodynamics
<number>
Colombier et al. Phys. Rev. B, 71, 165406 (2005)
Notes: <number>

## Slide 9
Disadvantages of hydrodynamics
<number>
No LTE on short times
Fluctuation of parameters
Large ratio of surface to volumetric energy for submicron objects
Kinetic process, nucleation, overheating etc.
Notes: <number>

## Slide 10
<number>
Molecular dynamics
Potential EAM
Velocity Verlet integration
Murray & Baskes Phys. Rev. B, 29, 6443 (1984)

## Slide 11
Molecular dynamics + TTM
<number>
Ivanov & Zhigilei, Phys. Rev. B, 68, 064114 (2003)
electrons
Notes: <number>

## Slide 12
Hydrodynamics and molecular dynamics
Potential EAM
EOS
<number>
Zhakhovskii et al. Appl. Surf. Sci. 255 (2009)
LAMMPS code
Notes: <number>

## Slide 13
Povarnitsyn et al., Appl. Surf Sci. 258 (2012)
Thermal conductivity & electron-ion coupling
<number>

## Slide 14
Laser energy absorption (Helmholtz equation)
<number>

## Slide 15: RF dielectric function for 400 and 800 nm
<number>

## Slide 16: Pump-probe technique
Widmann et al. Phys. Plasm. 8 (2001)
Pump
target
CCD
Probe
delay
<number>

## Slide 17: Diagnostics by s- and p-polarized pulses
Reflectivity dependence for s- and p-polarized probe beams
<number>
Povarnitsyn et al., Appl. Surf Sci. 258 (2012)
Phase shift for s- and polarized probe beams

## Slide 18: Equation of state (EOS) with metastable phases
bn
unstable
sp
<number>

## Slide 19: Nucleation model
<number>

## Slide 20: Expectation time for the gas bubble appearance
<number>

## Slide 21: Pressure profiles in target of Al, F = 2.6 J/cm2
50 ps
70 ps
100 пс
100 ps
Laser pulse
<number>

## Slide 22: MD simulation (incident F=1 J/cm2, Al)
<number>

## Slide 23
x-t diagram of density (incident F = 0.5 J/cm2)
<number>
RW
SW
melting
MD-TTM
Hydrodynamics

## Slide 24
x-t diagram of density (incident F = 2.0 J/cm2)
<number>
MD-TTM
Hydrodynamics

## Slide 25
<number>
x-t diagram of density (incident F = 4.0 J/cm2)
MD-TTM
Hydrodynamics

## Slide 26
<number>
x-t diagram of density (incident F = 20.0 J/cm2)
MD-TTM
Hydrodynamics

## Slide 27: Laser ablation experiment
target
<number>
 = 800 nm
 = 100 fs
F = 0.1 – 10 J/cm2

## Slide 28
<number>
Depth vs Fluence for 100 fs pulse, Al
experiment
simulation

## Slide 29
 | MD-TTM | HD-TTM
Time step | ~1 fs | ~1 fs
Space step | ~1 nm | ~1 nm
Run time | 8 houres, 360 cores | 1 min, 1 core
Nucleation | Potential-dependent | Nucleation model
Melting | Potential-dependent | Instant melting (EOS)
Condensation | Potential-dependent | Condensation model?
Phase states | Potential | EOS
Energy conservation | On average | Conservation laws
Ionization | Potential (T,Z)? | Ionization model
Comparison of MD-TTM and HD-TTM
<number>

## Slide 30: Ablation & nanoparticles (10M atoms, F=1 J/cm2, Al)
<number>

## Slide 31: Conclusions and outlook
We develop HD-TTM and MD-TTM approaches for simulation of laser ablation of metals
Wide-range models of optical and transport properties are used in both approaches
Ablation depth in experiment is close to the melted depth in simulation
MD-TTM underestimates the ablation depth (secondary splashing of metal is possible)
To do: more accurate models of nucleation and fragmentation in liquid and solid phases based on MD simulations
Posters for discussion
Open Access Tools for the Simulation of Ultrashort-Pulse Laser Ablation, Dr. Stefan Scharring, Institute of Technical Physics, German Aerospace Center (DLR)
Numerical Analysis of Ultrashort Laser Ablation: Application for Fabrication of Nanoparticles and Nanostructures, (M. Povarnitsyn JIHT RAS)
<number>